## Slide 1: Elena Echeverria Accelerator Physics Journal Club October 20/2022
PHOEBE
Current status and future work

## Slide 2: BIG THANKS!
Provide most of the information I will be presenting

## Slide 3: People
Jared Maxson
Chad Pennington
Vivek Anil
Maxson group
Shen group
Tomàs Arias
Arias group
J. Kevin Nangoi
Kyle Shen
Chris Parzyck
Hines group
Mellissa Hines
Will DeBenedetti
Jan Balajka
Alice Galdi
Hanjong Paik
Brendan Faeth
Luca Moreschini
Cheng Hu
Darrel Schlom
https://cbb.cornell.edu/ https://www.paradim.org/
Elena Echevarria

## Slide 4: Why?
GENERAL NEEDS
Reduce roughness of the alkali photocathodes
MTE measurements of single digit meV range
Photocathodes that work at ambient conditions
Better understanding of the effect of certain growth parameters on the alkali photocathodes performance
PHOEBE GOALS
Epitaxial growth of alkali antimonide compounds
MTE measurements on alkali antimonide compounds
Study the effects of protective coatings for photocathodes
Study the effect of the stoichiometry, crystal structure and/or temperature on the MTE measurements
To integrate the growth, characterization, and testing of these alkali photocathodes in vacuum

## Slide 5: Why Epitaxy?
Single crystalline photocathodes: epitaxy
Cs
flux
Sb
flux
Epitaxy is the growth of a crystal layer with one or more well-defined orientations with respect to an underlying crystal seed layer (usually a single crystal substrate)
Substrate
Epitaxial
layer
Epitaxial single-oriented films would allow:
Roughness control
Orientation control  surface potential control
Measurements of intrinsic properties (optical constants, band structure, intrinsic MTE…)
Choose the method: MBE
Select suitable substrates
Identify suitable growth conditions
reaction-interdiffusion
adsorption
diffusion
nucleation
re-evaporation

## Slide 6: Choosing the method
Cs/In
Sb
Substrate
heater
QMB
Cs
Sb
Substrate
heater
Current
Light source
QMB
RHEED
Typical photocathode growth: Photocurrent monitored
Quantum efficiency oriented
Our growth method:
RHEED monitored
Structure oriented
Light source

## Slide 7: Choosing the substrate
<100>
Sb3-
Cs+
4 X SiC (a=0.436 nm)
1 X Cs3Sb (a=0.9165 nm)
≈
Jack and Wachtel (1957)
2x Sb +2x Cs
4x Cs
2x Sb +2x Cs
4x Cs
Based on previous studies, 3C-SiC has been the selected substrate (but also tested: TiO2 , MgF2)
A Galdi, et al. Applied Physics Letters 118 (24), 244101
Some work from John Medley and Mengjia Gaowei at BNL has shown better reproducibility on Gr/4H-SiC…Something to explore in the future

## Slide 8: Growth Conditions: Temperature
Cs-Sb co-deposition on SiC substrate
Polycrystalline
Rough
Fiber texture
Flat
Low crystallinity
Rough
λ=504 nm
Lower Growth Temperature
Improved Quantum Efficiency
Polycrystalline Films
High Growth Temperature
Improved Crystal Order
OOP Film Orientation
Reduced Surface Roughness
Reduced Quantum Efficiency

## Slide 9: Solid Phase (Molecular Beam) Epitaxy
Time
Low Deposition temperature to take advantage of improved Cs sticking coefficient
High temperature Cs anneal to improve crystallinity
Temp
T=40°C
Cs
Sb
Deposition
Cooling
T=85°C
Crystall.
Annealing

## Slide 10: Results: Epitaxial Cs3Sb Growth!
SiC [10]
Cs3Sb [10]
Cs3Sb [11]
SiC [11]
Φ=0°
Φ=45°
e-
e-

## Slide 11: PHOBE Design in Newman
The cryogenic TE meter is in the same room as the growth system
A laser system is hosted in the adjacent room and light is delivered to the TE meter
Fume Hood and glove box in the same room for sample/sources preparation
Cryogenic TE meter
Photocathode MBE
New Laser room!
Fume Hood
Glove Box

## Slide 12: Compatible sample holders
Universal sample holder:
Cryogenic TE meter (Maxson group)
STM/XPS (Hines group)
MBE/ARPES ( PARADIM, Shen group)
Crossplatform sample holder:
STM/XPS (Hines group)
MBE/ARPES (PARADIM, Shen group)
Standard Omicron with pocket:
STM/XPS (Hines group)
Currently working on a design for the gun miniplug holder

## Slide 13: What do we have?
TE-Meter
Solenoid Scans
Cryogenic capabilities
Emittance Measurement System (EMS)

## Slide 14: What do we have?
Suitcase
Sample carrier with 4 slots for omicron plates style holders
Easy sample transfer between systems
QE measurements setup

## Slide 15: What do we have?
MBE System
RHEED
Storage chamber
Loadlock
Transfer chamber
Growth module with 8 source ports
Vacuum suitcase connection cross
QE meas. station
Sources: Cs, Sb, Mg, Cr
RHEED
Storage chamber with room to keep up to 10 samples
QE measurements and spectral response
Co-deposition and epitaxial growth

## Slide 16: Epitaxial Cs3Sb at PHOBE
Epitaxial growth demonstrated at PHOBE… not surprising but it also lead to the discovery of a new phase of Cs-Sb photocathode…

## Slide 17: Optical interference in the substrate
Photocathode film: <10 nm thickness
Si ~ 0.5 mm
3C-SiC(100) ~ 1.3 um
How can we exploit interference effects to improve cathode performance?
Enhanced photocathode performance through optimization of film thickness and substrate
Journal of Vacuum Science & Technology B 35, 022202 (2017); https://doi.org/10.1116/1.4976527

## Slide 18: CsSb photocathode
X-ray Photoemission Spectroscopy (XPS) confirms the presence of CsSb phase
Scanning Tunneling Microscopy (STM) shows roughness of 0.8 nm
RHEED pattern which is different from Cs3Sb
Not angle dependence – fiber textured surface with flat regions

## Slide 19: Why we care about CsSb?
Spectral response of CsSb reveals an emission threshold near 580 nm and QE of 1% at 400 nm
CsSb is very robust to oxygen exposure by over two order of magnitude compared to other Cs-Sb compounds.

## Slide 20: Conclusions
Lab up and running  Plenty of work to do!
PHOEBE can produce photocathodes by co-depositon or molecular beam epitaxial methods with high throughput
  PARADIM experiments: 59 samples grown in 27 days (operating 24/7)
  PHOBE: 92 Cs-Sb samples grown from October 2021 (+ Other photocathodes 120 total)
A new Cs-Sb phase has been identified (CsSb) which is robust under oxygen conditions

## Slide 21: Future Directions
New sources (Na, K…)
Stoichiometry dependence on the MTE (CsSb vs Cs3Sb)
Temperature dependence measurements on the TE-Meter system
Epitaxial vs Co-deposition for MTE measurements (Crystal dependence studies)
Better characterization of the cathodes at the beginning of the growth (Do we have CsSb and then Cs3Sb?)

## Slide 22: Holders